Heat press setting:

- Preheat the heat press to 305°F (150°C).

- Place your fabric onto the heat press and preheat it for 5-10 seconds to remove any moisture and wrinkles.

- Place your design onto the fabric, with the carrier sheet facing up.

- Apply heat and pressure for 10-15 seconds using medium to high pressure.

- Peel off the carrier sheet while it is Cold.

- If the vinyl is not fully adhered, repeat steps 4-5 until it is.

Iron-On setting:

- For using a household iron, set it to the Cotton/Linen or Wool setting, which is usually the highest temperature setting available.

- Turn OFF the steam setting on the iron.

- Preheat the area of the fabric where you want to apply the vinyl for 10-15 seconds.

- Place the weeded image onto the preheated fabric, liner side up. Apply medium to high pressure with the iron for 25-30 seconds, pressing down firmly and evenly with both hands.

- Flip the fabric over and apply medium pressure with the iron to the back of the material for an additional 25-30 seconds.

- Let the vinyl cool for a few seconds, then gently peel off the carrier sheet while it is still Cold.

- If the vinyl is not fully adhered, repeat steps 4-6 until it is.

Care Instructions

Wait 24 hours before washing. Handwash the embellished item inside out in cold water. Do not bleach. Do not tumble dry. If necessary, iron back side of the garment.

Following these care instructions will help to preserve the quality and longevity of your heat transfer vinyl project.